Chip back potential is the level which bulk silicon is maintained by on-chip connection, or it is the level to which the chip back must be connected when specifically stated below. If no potential is given the chip back should be isolated.

.018”

E

B

.015”

CHIP BACK IS COLLECTOR

Top Material: Al

Backside Material: Au

Bond Pad Size:  .004” Min.

Backside Potential: Collector

Mask Ref: 004842

APPROVED BY: DK 			DIE SIZE .015” X .018” 	                   DATE:  10/18/21

MFG: NATIONAL SEMI                       	   THICKNESS .008”                                     P/N: 2N3904

DG 10.1.2

#### Rev B, 7/19/02